SGS胶带测试——压敏胶带通用测试

Universal Test Methods for Pressure-Sensitive Tapes

Total Thickness  总厚度

ASTM D3652-01

Thickness of Adhesive  胶粘层厚度

ASTM D3652-01

Thickness of Liner   基材厚度

ASTM D3652-01

Width   宽度

ASTM D5750-95(2001)

Length   长度

ASTM D5750-95(2001)

Unwind Force   解卷力

ASTM D3811-96

Tack(rolling ball method)   初粘性 （滚球法）

ASTM D3121-06, GB 4852-2002

Peel Adhesion at 180°    180°剥离强度

ASTM D3330-04, GB 2792-1998

Peel Adhesion at 90°   90°剥离强度

ASTM D3330-04

Holding Power   持粘性

ASTM D3654-066, GB 4851-1998

Tensile Strength   拉伸强度

ASTM D3759-05, GB 7753-87

Elongation   断裂伸长率

ASTM D3759-05, GB 7753-87

Water Penetration Rate    水渗透率

ASTM D3816-96(2003), GB 15330-94

Water Vapor Transmission     水蒸气透过性

ASTM D3833-96(2001), GB 15331-94

Adhesion to Fiberboard    对纤维板的持粘性

ASTM D2860-04

Accelerated Weathering by Xenon-Arc Exposure   氙灯加速老化

ASTM D6551-05

Accelerated Weathering by Carbon-Arc Exposure   碳弧光加速老化测试

ASTM D3815-05

Water Resistance     耐水性

ASTM D5570-94

Accelerated aging   加速老化测试

ASTM D3611-06

Pb,Cd,Hg,Cr6+

Content   包装材料环保测试

SGS胶带测试——电子电气用压敏胶带的标准测试

ASTM D1000-04

Standard Test Method for Pressure-Sensitive Adhesive-Coated

Overall thickness 总厚度

ASTM D1000-04

Length of tape in a roll  卷长

ASTM D1000-04

Tensile breaking strength  拉伸断裂强度

ASTM D1000-04

Elongation   断裂伸长率

ASTM D1000-04

Adhesion strength to steel   剥离强度（对钢板）

ASTM D1000-04

Adhesion strength to backing   剥离强度（对基材）

ASTM D1000-04

Flagging  翘边测试

ASTM D1000-04

Thermosetting Properties  热硬化性能

ASTM D1000-04

Dielectric Breakdown Test   击穿电压

ASTM D1000-04, ASTM D149-97

Effect of Accelerated Aging on Dielectric Breakdown Voltage for High-Temperature Tape

耐高温胶 带的热老化测试

ASTM D1000-04, ASTM D149-97

Flammability  阻燃性

ASTM D1000-04

Bond Strength after Solvent Immersion   溶剂浸泡后的粘合强度

ASTM D1000-04

Oil Resistance   耐油性

ASTM D1000-04

Resistance to Accelerated Aging(Heat and Moisture)  耐温湿老化

ASTM D1000-04

SGS胶带测试——聚氯乙烯、聚乙烯和橡胶绝缘胶带

UL 510-05

Polyvinyl Chloride, Polyethylene, and Rubber Insulating Tape

For all tapes:

Sunlight resistance test (carbon arc)  耐候性测试（碳弧灯）

UL 510-05 (for 100hrs)

For thermoplastic tape:Overall thickness    总厚度

UL 510-05

Tensile Breaking Strength   拉伸断裂强度

UL 510-05, ASTM D1000-04

Elongation   断裂伸长率

UL 510-05, ASTM D1000-04

Dielectric Breakdown Test   击穿电压

UL 510-05, ASTM D1000-04

Adhesion Strength   剥离强度（对不锈钢板或基材）

UL 510-05, ASTM D1000-04

Moisture Absorption Test    耐湿测试

UL 510-05, ASTM D1000-04

Exposure to Heat Test  耐热测试

UL 510-05

Exposure to Cold Test   耐寒测试

UL 510-05

Deformation Test        变形测试

UL 510-05

Storage Test                储存测试

UL 510-05

For rubber tape:Tensile Strength    拉伸强度

UL 510-05, ASTM D412-06

Elongation   断裂伸长率

UL 510-05, ASTM D412-06

Storage Test    储存测试

UL 510-05

Dielectric Breakdown Test   介电击穿电压

UL 510-05